## Slide 1
Layered Double Hydroxides for Circular Phosphorus use in Agriculture
Dr. Maarten Everaert
FERTASA Soil Fertility and Plant Nutrition Symposium
September 28, 2023

## Slide 2
INTRODUCTION
P fertilizers and rock phosphate
Mined apatite rock material  non-renewable
Transformed into soluble P fertilizers
  TSP, DAP, MAP (soluble P)
P reserves will last at least another 200 years (2023)
Africa Capital Digest

## Slide 3
INTRODUCTION
Towards sustainable P use
Intensive mining practices
Egyptra

## Slide 4
INTRODUCTION
Towards sustainable P use
Intensive mining practices
Access to rock P or P fertilizers on local scale
PJ De Bauw

## Slide 5
INTRODUCTION
Towards sustainable P use
Intensive mining practices
Access to rock P or P fertilizers on local scale
Environmental quality
EWG

## Slide 6
INTRODUCTION
Towards sustainable P use
Intensive mining practices
Access to rock P or P fertilizers on local scale
Environmental quality
EWG
  Improve the P use efficiency
  Increase the use of alternative sources of P

## Slide 7
INTRODUCTION
Layered double hydroxides (LDHs)
= Inorganic anion exchange materials: divalent (Mg2+) and trivalent (Al3+) metal hydroxide layers and a negatively charged anion interlayer
Structurally relates to brucite Mg(OH)2

## Slide 8
INTRODUCTION
Layered double hydroxides (LDHs)
= Inorganic anion exchange materials: divalent (Mg2+) and trivalent (Al3+) metal hydroxide layers and a negatively charged anion interlayer
Structurally relates to brucite Mg(OH)2
Introduction of trivalent cations (Al3+)
→ positively charged layers

## Slide 9
INTRODUCTION
Layered double hydroxides (LDHs)
= Inorganic anion exchange materials: divalent (Mg2+) and trivalent (Al3+) metal hydroxide layers and a negatively charged anion interlayer
Structurally relates to brucite Mg(OH)2
Introduction of trivalent cations (Al3+)
→ positively charged layers
→ anion exchange capacity
→ exchangeable anions in interlayer
LDH have a high affinity for PO4 anions
→ adsorbent for PO4
→ P desorption and reuse of LDHs questionable
interlayer spacing
d spacing

## Slide 10
INTRODUCTION
LDHs for circular P use in agriculture
CENTRAL IDEA
Cl
Cl
Cl anion
PO4 anion
CO3 anion

## Slide 11
INTRODUCTION
LDHs for circular P use in agriculture
CENTRAL IDEA
Cl
Cl
Cl anion
PO4 anion
CO3 anion
Release mechanisms of P from LDH, the effectiveness of powdered LDH as fertilizer
LDH application form determines the slow-release character of P-LDH
P-LDHs and limiting P losses to the environment
EXPERIMENTS

## Slide 12
INTRODUCTION
EXPERIMENTS
1
Chart: t (h)
| 0.1 | 1 | 3 | 24 | 72 | 216 | 649 | 2400
KH2PO4 | 0 | 0.51057 | 0.69657 | 0.92179 | 0.92659 | 0.92699 | 0.92762 | 0.92762
TSP | 0 | 0.43693 | 0.66645 | 0.87732 | 0.88833 | 0.8917 | 0.89431 | 0.89459
Mg-Al (2/1) | 0 | 0.037989 | 0.19131 | 0.3893 | 0.44713 | 0.50958 | 0.54758 | 0.55082
KH2PO4
TSP
P-LDH
1. P release mechanisms and powder LDH fertilizer
P-LDHs are sparingly-soluble in water
1. Neutral/alkaline conditions
P release via anion exchange (carbonate) supply from soil
2. Acid conditions
LDH dissolution  P release + liming effect
LDH incubation in 2 mM carbonate solution (pH 8)
Released P is captured with anion exchange membranes
CENTRAL IDEA

## Slide 13
INTRODUCTION
EXPERIMENTS
1
2 soils: acid-weathered soil (Kenya) and calcareous soil (Spain)
2 fertilizers: P-LDH and KH2PO4, mixed in the soil as powder at varying doses
Soils were used for growth of barley
Chart: Added P dose (mg-P kg-1)
| 0 | 0 | 0 | 10 | 10 | 10 | 30 | 30 | 30 | 100 | 100 | 100 | 300 | 300 | 300
P-LDH | 0.15 | 0.16 | 0.11 | 0.2 | 0.17 | 0.17 | 0.15 | 0.13 | 0.21 | 0.9 | 0.97 | 0.93 | 2.59 | 2.6 | 2.46
KH2PO4 | 0.15 | 0.16 | 0.11 | 0.14 | 0.16 | 0.12 | 0.09 | 0.11 | 0.17 | 0.16 | 0.16 | 0.18 | 0.71 | 0.68 | 0.49
KH2PO4 average | 0.14 | 0.14 | 0.12333 | 0.16667 | 0.62667
P-LDH average | 0.14 | 0.18 | 0.16333 | 0.93333 | 2.55
Chart: Added P dose (mg-P kg-1)
| 0 | 0 | 0 | 10 | 10 | 10 | 30 | 30 | 30 | 100 | 100 | 100 | 300 | 300 | 300
P-LDH | 0.29 | 0.2 | 0.32 | 0.58 | 0.48 | 0.52 | 0.9 | 0.96 | 0.97 | 1.21 | 1.24 | 1.53 | 0.79 | 1.78 | 1.02
KH2PO4 | 0.29 | 0.2 | 0.32 | 0.46 | 0.44 | 0.63 | 0.82 | 0.75 | 0.85 | 1.72 | 1.68 | 1.66 | 2.47 | 3.04 | 1.81
KH2PO4 average | 0.27 | 0.51 | 0.80667 | 1.6867 | 2.44
P-LDH average | 0.27 | 0.52667 | 0.94333 | 1.3267 | 1.1967
*
*
*
*
*
P-LDH
KH2PO4
acid-weathered soil
calcareous soil
P-LDH
KH2PO4
CENTRAL IDEA
1. P release mechanisms and powder LDH fertilizer

## Slide 14
INTRODUCTION
EXPERIMENTS
1
2 soils: acid-weathered soil (Kenya) and calcareous soil (Spain)
2 fertilizers: P-LDH and KH2PO4, mixed in the soil as powder at varying doses
Soils were used for growth of barley
Chart: Added P dose (mg-P kg-1)
| 0 | 0 | 0 | 10 | 10 | 10 | 30 | 30 | 30 | 100 | 100 | 100 | 300 | 300 | 300
P-LDH | 0.15 | 0.16 | 0.11 | 0.2 | 0.17 | 0.17 | 0.15 | 0.13 | 0.21 | 0.9 | 0.97 | 0.93 | 2.59 | 2.6 | 2.46
KH2PO4 | 0.15 | 0.16 | 0.11 | 0.14 | 0.16 | 0.12 | 0.09 | 0.11 | 0.17 | 0.16 | 0.16 | 0.18 | 0.71 | 0.68 | 0.49
KH2PO4 average | 0.14 | 0.14 | 0.12333 | 0.16667 | 0.62667
P-LDH average | 0.14 | 0.18 | 0.16333 | 0.93333 | 2.55
Chart: Added P dose (mg-P kg-1)
| 0 | 0 | 0 | 10 | 10 | 10 | 30 | 30 | 30 | 100 | 100 | 100 | 300 | 300 | 300
P-LDH | 0.33 | 0.22 | 0.27 | 0.27 | 0.3 | 0.39 | 0.64 | 0.48 | 0.48 | 0.75 | 0.96 | 0.81 | 1.88 | 2.79 | 2.29
KH2PO4 | 0.33 | 0.22 | 0.27 | 0.21 | 0.23 | 0.29 | 0.34 | 0.35 | 0.51 | 0.75 | 1.06 | 0.95 | 1.85 | 1.68 | 1.71
KH2PO4 average | 0.27333 | 0.24333 | 0.4 | 0.92 | 1.7467
P-LDH average | 0.27333 | 0.32 | 0.53333 | 0.84 | 2.32
Chart: Added P dose (mg-P kg-1)
| 0 | 0 | 0 | 10 | 10 | 10 | 30 | 30 | 30 | 100 | 100 | 100 | 300 | 300 | 300
P-LDH | 0.29 | 0.2 | 0.32 | 0.58 | 0.48 | 0.52 | 0.9 | 0.96 | 0.97 | 1.21 | 1.24 | 1.53 | 0.79 | 1.78 | 1.02
KH2PO4 | 0.29 | 0.2 | 0.32 | 0.46 | 0.44 | 0.63 | 0.82 | 0.75 | 0.85 | 1.72 | 1.68 | 1.66 | 2.47 | 3.04 | 1.81
KH2PO4 average | 0.27 | 0.51 | 0.80667 | 1.6867 | 2.44
P-LDH average | 0.27 | 0.52667 | 0.94333 | 1.3267 | 1.1967
*
*
*
*
*
P-LDH
KH2PO4
acid-weathered soil
acid-weathered soil + gypsum
calcareous soil
P-LDH
KH2PO4
P-LDH
KH2PO4
CENTRAL IDEA
1. P release mechanisms and powder LDH fertilizer

## Slide 15
INTRODUCTION
EXPERIMENTS
2. LDH application form and slow P release
1
2
1. Powder application: limited effect of fertilizer type
2. Granule application:
acid-weathered soil
pH neutral soil
calcareous soil
CENTRAL IDEA

## Slide 16
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 3.9547 | 1.249 | 4.2675 | 0.9435 | 4.426 | 5.8328 | 0.61167
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.24 | 0.23981 | 0.24 | 0.23971 | 0.24 | 0.24 | 0.23311
Pdfsoil | 0.66677 | 0.35749 | 0.9052 | 0.38061 | 0.82677 | 0.20289 | 0.42923
Pdff | 4.1584 | 1.0322 | 4.0525 | 0.83048 | 4.7742 | 8.0757 | 0
acid-weathered soil
calcareous soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 17
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 18
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 19
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
P available for plants
P in the fertilizer
SOIL
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 20
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
POWDER
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 21
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
POWDER
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 22
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
GRANULAR
SOLUBLE
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 23
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
GRANULAR
SOLUBLE
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 24
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
GRANULAR
SLOW-RELEASE
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 25
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
GRANULAR
SLOW-RELEASE
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 26
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
GRANULAR
SLOW-RELEASE
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
acid-weathered soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 27
INTRODUCTION
EXPERIMENTS
1
2
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 0.26425 | 0.28825 | 0.1835 | 0.268 | 0.17 | 1.3785 | 0.072667
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: DMY (g/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
DMY | 3.9547 | 1.249 | 4.2675 | 0.9435 | 4.426 | 5.8328 | 0.61167
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.199 | 0.17186 | 0.1679 | 0.17882 | 0.14042 | 0.23957 | 0.066812
Pdfsoil | 0.085676 | 0.016787 | 0.0402 | 0.0090422 | 0.023878 | 0.053183 | 0.0034867
Pdff | 0.074457 | 0.12453 | 0.03561 | 0.10112 | 0.022861 | 1.4325 | 0
Chart: P uptake (mg/pot)
| pwd | gran | pwd | gran | pwd | gran | LDH | struvite | MAP | ctr
Pdfseed | 0.24 | 0.23981 | 0.24 | 0.23971 | 0.24 | 0.24 | 0.23311
Pdfsoil | 0.66677 | 0.35749 | 0.9052 | 0.38061 | 0.82677 | 0.20289 | 0.42923
Pdff | 4.1584 | 1.0322 | 4.0525 | 0.83048 | 4.7742 | 8.0757 | 0
acid-weathered soil
calcareous soil
CENTRAL IDEA
2. LDH application form and slow P release

## Slide 28
INTRODUCTION
EXPERIMENTS
3. P-LDHs limit P losses to environment
1
2
3
Trays with poor P fixing soil, grass cover
4 treatments: granules of P-LDH, struvite or MAP are broadcasted on soil surface (40 kg P ha-1) + control (no P)
Trays placed in a calibrated rain cabin on specific moments after P application (day 1, 5, 15 and 30 after P application) and sprayed upon (rate ~98 mm h-1)
Runoff water collected: amount of runoff water per tray recorded
P analysis on filtered samples from runoff water
CENTRAL IDEA

## Slide 29
3. P-LDHs limit P losses to environment
Chart: P losses (% of applied P)
MAP | 0.088093 | 0.21416 | 0.3501 | 0.40497 | 0.41558 | 0.41994
LDH | 0.0021681 | 0.0052845 | 0.0092459 | 0.016834 | 0.021167 | 0.023624
Struvite | 0.0012622 | 0.0029464 | 0.0052105 | 0.010739 | 0.015579 | 0.019426
Control | 0.00051803 | 0.0011702 | 0.001904 | 0.0030195 | 0.0039382 | 0.0046117
Chart: P losses (% of applied P)
| 5 min | 15 min | 30 min | 5 days | 15 days | 30 days
LDH | 0.0021681 | 0.0052845 | 0.0092459 | 0.016834 | 0.021167 | 0.023624
Struvite | 0.0012622 | 0.0029464 | 0.0052105 | 0.010739 | 0.015579 | 0.019426
Control | 0.00051803 | 0.0011702 | 0.001904 | 0.0030195 | 0.0039382 | 0.0046117
MAP
LDH
struvite
control
INTRODUCTION
EXPERIMENTS
CENTRAL IDEA
1
2
3

## Slide 30
INTRODUCTION
EXPERIMENTS
CENTRAL IDEA
CONCLUSIONS
Conclusions
P release from LDH by anion exchange (pH neutral, alkaline) or LDH dissolution (acid)
Powdered LDH is a relatively fast-working fertilizer, with good effectiveness in calcareous soils and less strongly P-fixing soils
Granulation of LDH  slow-release fertilizer
Slow release of P from LDH does not increase P uptake in strongly P-fixing soils
 In acid-weathered soils, a local P saturation is required: granular soluble P
Slow-release P fertilizers are a tool to limit losses of P to the environment

## Slide 31
Future challenges
P recycling with LDHs: cost-effectiveness, materials for LDH production, field trial
INTRODUCTION
EXPERIMENTS
CENTRAL IDEA
CONCLUSIONS

## Slide 32
Future challenges
P recycling with LDHs: cost-effectiveness, materials for LDH production, field trial
LDHs and other nutrients
INTRODUCTION
EXPERIMENTS
CENTRAL IDEA
CONCLUSIONS
N: NO3-
Zn: Zn2+
B: B(OH)4-
Mo: MoO42-

## Slide 33
Acknowledgements
Prof. Erik Smolders
Prof. Dirk De Vos
Prof. Mike McLaughlin
Prof. Roel Merckx
Dr. Fien Degryse
Dr. Rodrigo Coqui da Silva
Dr. Kris Dox

## Slide 36
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
LDH synthesis via coprecipitation:
  Addition of Mg and Al nitrate solution
  pH control
Different LDHs were obtained by varying
  Solution molar Mg/Al ratio
  Synthesis pH
PO4 uptake tested
  Batch reactions
  Adsorption isotherms
Synthesis and PO4 exchange

## Slide 37
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 0 | 3.6545231691774194E-4 | 0 | 0.87105016094032262 | 2.9064784442258063 | 7.3022284294516124 | 11.578938568564515 | 16.258306039516128
LDH12(2) | 0 | 0.40452 | 0.56533 | 1.2639 | 1.3792 | 1.5348 | 1.5284 | 1.7654
LDH12(3) | 0 | 0.17364 | 0.47148 | 0.97353 | 1.0698 | 1.2095 | 1.2776 | 1.4567
LDH12(4) | 0.14993 | 0.35988 | 0.49778 | 0.48824 | 0.57842 | 0.62857 | 0.69361
LDH(2/1)
Synthesis and PO4 exchange

## Slide 38
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 0 | 3.6545231691774194E-4 | 0 | 0.87105016094032262 | 2.9064784442258063 | 7.3022284294516124 | 11.578938568564515 | 16.258306039516128
LDH12(2) | 0 | 0.40452 | 0.56533 | 1.2639 | 1.3792 | 1.5348 | 1.5284 | 1.7654
LDH12(3) | 0 | 0.17364 | 0.47148 | 0.97353 | 1.0698 | 1.2095 | 1.2776 | 1.4567
LDH12(4) | 0.14993 | 0.35988 | 0.49778 | 0.48824 | 0.57842 | 0.62857 | 0.69361
LDH (2/1)
LDH(2/1)
Synthesis and PO4 exchange

## Slide 39
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 0 | 3.6545231691774194E-4 | 0 | 0.87105016094032262 | 2.9064784442258063 | 7.3022284294516124 | 11.578938568564515 | 16.258306039516128
LDH12(2) | 0 | 0.40452 | 0.56533 | 1.2639 | 1.3792 | 1.5348 | 1.5284 | 1.7654
LDH12(3) | 0 | 0.17364 | 0.47148 | 0.97353 | 1.0698 | 1.2095 | 1.2776 | 1.4567
LDH12(4) | 0.14993 | 0.35988 | 0.49778 | 0.48824 | 0.57842 | 0.62857 | 0.69361
LDH(2/1)
LDH(3/1)
LDH(3/1)
Synthesis and PO4 exchange

## Slide 40
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 0 | 3.6545231691774194E-4 | 0 | 0.87105016094032262 | 2.9064784442258063 | 7.3022284294516124 | 11.578938568564515 | 16.258306039516128
LDH12(2) | 0 | 0.40452 | 0.56533 | 1.2639 | 1.3792 | 1.5348 | 1.5284 | 1.7654
LDH12(3) | 0 | 0.17364 | 0.47148 | 0.97353 | 1.0698 | 1.2095 | 1.2776 | 1.4567
LDH12(4) | 0.14993 | 0.35988 | 0.49778 | 0.48824 | 0.57842 | 0.62857 | 0.69361
LDH(2/1)
LDH(3/1)
LDH(4/1)
LDH(4/1)
Synthesis and PO4 exchange

## Slide 41
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 2.2154882154882156E-3 | 3.3232323232323235E-3 | 7.3111111111111113E-2 | 1.909750841750842 | 4.5849528619528623 | 13.074703703703705
LDH12(2) | 0 | 0.23994 | 0.67005 | 0.82911 | 0.91854 | 1.2829
LDH10(2) | 0 | 0.22817 | 0.66411 | 1.2582 | 1.4419 | 1.7634
LDH(pH12)
PO43-
Synthesis and PO4 exchange

## Slide 42
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 2.2154882154882156E-3 | 3.3232323232323235E-3 | 7.3111111111111113E-2 | 1.909750841750842 | 4.5849528619528623 | 13.074703703703705
LDH12(2) | 0 | 0.23994 | 0.67005 | 0.82911 | 0.91854 | 1.2829
LDH10(2) | 0 | 0.22817 | 0.66411 | 1.2582 | 1.4419 | 1.7634
LDH(pH12)
LDH(pH12)
PO43-
Synthesis and PO4 exchange

## Slide 43
INTRODUCTION
EXPERIMENTS
HYPOTHESIS
1
Chart: PO4 concentration (mM)
| 2.2154882154882156E-3 | 3.3232323232323235E-3 | 7.3111111111111113E-2 | 1.909750841750842 | 4.5849528619528623 | 13.074703703703705
LDH12(2) | 0 | 0.23994 | 0.67005 | 0.82911 | 0.91854 | 1.2829
LDH10(2) | 0 | 0.22817 | 0.66411 | 1.2582 | 1.4419 | 1.7634
LDH(pH10)
LDH(pH12)
LDH(pH10)
HPO42-
Synthesis and PO4 exchange